VBRA TECHNICAL BULLETIN – No 5

RESISTANCE SPOT WELDING CHECKLIST

Modern motor cars using New Generation Steels (UHSS, AHSS & Boron), require Bodyshops to take care in using the correct repair methods and welding equipment, this in turn means that good practice and methods should be used to ensure consistent repair quality.

This is part of the of the industry standard PAS125, It is necessary to collate certain information on an ongoing basis during the process of Resistance Spot Welding.

It is not a requirement of PAS125 that a bodyshop should have a welder that records each weld and its parameters; however, it is desirable that certain key information is checked and recorded to ensure correct working practices and operation of your Resistance Spot Welder, along with the Repair Method for each structural repair.

Certain procedures should be carried out before commencing each Structural repair, the check list aims to guide and assist you in meeting these requirements.

The type of welder is secondary to the checks that must be carried out before starting any structural repair that entails Spot welding.

(MAY 2008)